## Slide 1
X-ray Tomographic Systems for Cultural Heritage
Maria Pia Morigi
Department of Physics and Astronomy «Augusto Righi» (DIFA)
University of Bologna
Bologna, July 19, 2023
SUMMER SCHOOL
PHYSICAL SENSING AND PROCESSING

## Slide 2
Application of scientific methods and technologies to Cultural Heritage study
Science & Cultural Heritage
WHAT material is it made of?
WHEN was it made?
WHERE was it made?
HOW was it made?
HOW can we preserve it for future generations?

## Slide 3
X-ray Computed Tomography (CT) is a powerful non-destructive diagnostic technique, able to give morphological and physical information on the inner structure of the object studied, overcoming an important limit of radiography: the superimposition of elements belonging to different layers of the object.
“Tomography” comes from the Greek word “tómos”, that means “section”. In fact this kind of non-destructive analysis is used to “virtually” cut an object and see inside it.
X-ray Computed Tomography

## Slide 4
I(x) = I0e-mx
Attenuation of monochromatic X-ray photons
Beer-Lambert’s law for homogeneous material and monochromatic photons:
where:
I is the number of photons reaching the detector in presence of the test material
I0 is the number of photons that would be detected without the test material
m is the linear attenuation coefficient for a homogeneous material
x is the thickness of the test material.

## Slide 5: Attenuation of monochromatic X-ray photons
m depends on:
the density of the material
the atomic number of the material
the energy of the X-ray beam
copper
stone
water
wood
X-ray attenuation (I/I0) in different materials.
60 keV
100 keV
30 keV
water
E=100 keV
Attenuation in water of monochromatic X-rays for different X-ray energies.

## Slide 6
The first CT scanner for clinical use ("EMI Mark I scanner") was developed by the British engineer Godfrey Hounsfield in the research laboratories of EMI (United Kingdom) and installed in 1971 at Atkinsons Morley's Hospital in Wimbledon (London).
.
The first CT scanner (1971)
In 1979 Hounsfield shared the Nobel Prize for Medicine with the physicist Allan Cormack.

## Slide 7
Tomographic slices
A tomographic slice is the image of a cross-section of the object under investigation, in which the grey-levels are proportional to the values of the linear attenuation coefficient in that section of the object.

## Slide 8
The measurement process (first generation CT scannes)
Principle of the first CT scanner, developed by Hounsfield and designed to study the human brain.
An X-ray tube emitting a pencil-like beam is coupled to a single radiation detector. The two are moved together on a carriage, so that a plane in the head is scanned by a series of parallel rays as the translation takes place. For each ray the fraction of the radiation transmitted is measured and stored in a computer.

## Slide 9
The measurement process
The pencil beam of X-rays is translated across the patient to acquire a projection, that is made up of a large number of pencil-beam attenuation measurements.
The X-ray source and the detector are rotated around the patient and a large number of projections are acquired, each one at a different angle.

## Slide 10
Assuming that the X-ray beam is monoenergetic and has an incident intensity I0, then the intensity I1 of the beam transmitted through a small volume of tissue having thickness x and attenuation coefficient m1 is:
In traversing from one side of the patient to the other, the X-ray beam will be attenuated by all the voxels through which it passes. The emerging X-ray beam will have an intensity I given by:
The measurement process

## Slide 11
The figure shows the measured X-ray intensities and the corresponding logarithms of the intensity ratios I0/I for one projection.
Attenuation profile
Intensity profile
The measurement process

## Slide 12
The measurement process
The image shows a cross-sectional view of the object under investigation superimposed upon a rectangular matrix of pixels, which for clarity of presentation has been made very coarse.
The elements of lenght l(x,y) are determined by the geometry of the system and hence can be calculated and stored in the computer.
Let m(x,y) be the average attenuation coefficient of the tissues in the pixel (x,y). The radiation transmitted It is related to the incident radiation I0 by:

## Slide 13
Our problem is to determine the attenuation coefficient of the object under investigation in each picture element of the slice.
The measurement process
The reconstruction process creates an image that is a map of the X-ray attenuation coefficients of the object in the plane under examination.

## Slide 14
Image reconstruction
The method used on most of the CT scanners is the method of filtered back-projection. The mathematics of filtered back-projection dates back to 1917 with the work of the Austrian mathematician Radon, who theoretically solved the problem of obtaining a section of an object using an infinite set of rays passing through it.
However, as previously stated, it was not until the 1960s that two scientists, the engineer Geoffrey Hounsfield and the physicist Allan Cormack (separately) succeeded in obtaining the section of an object experimentally.

## Slide 15
Image reconstruction: simple back-projection
Back-projection reconstructs an image by taking each view and smeraing it along the path it was originally acquired. The resulting image is a blurry version of the correct image.

## Slide 16
The image reconstruction process of the FBP algorithm. Each set of projection data, taken at different angles, undergoes convolution filtering before back-projection. This removes the blurring that would result from simple back-projection without filtering.
Image reconstruction: filtered back-projection

## Slide 17
Filtered Back-Projection
Japanese helmet fromn the Stibbert Museum (Florence).

## Slide 18
Components of a CT scanner
Computed Tomography implies
a radiation source
a detection system
mechanics
control software
5. reconstruction and rendering software

## Slide 19
mm
cm
m
X-ray CT & Cultural Heritage
DIFFERENT SIZE
Increasing size
X-ray CT & Cultural Heritage

## Slide 20
Paper
Low energy
Wood
Medium energy
Stone
Metals
High energy
X-ray CT & Cultural Heritage
Increasing energy

## Slide 21
X-ray CT & Cultural Heritage
It is difficult to move the works of art from the place where they are kept.
Therefore it is important to develop equipment that is easy to move, specifically designed for Cultural Heritage analysis on-site.
In the recent past, our research group developed a number of acquisition systems for Digital Radiography and Computed Tomography. We have performed high resolution micro-CT of small objects (voxel size of few microns) and CT of large works of art (up to 2 m of size), using different kinds of X-ray sources and different setups, in order to meet the different needs of various case studies.

## Slide 22
Micro-CT
CT system for large-size objects
CT system for medium-size objects
X-ray CT & Cultural Heritage

## Slide 23
X-ray CT & Cultural Heritage
slice to
rendering 3D

## Slide 24
Examples of case-studies
Micro-CT analysis of small samples

## Slide 25
Micro-CT system

## Slide 26
X-ray detector
Photonics Science liquid cooled camera CCD Kodak sensor 4008x2672 pixels; pixel size: 9 mm; FOV = 36 x 24 mm2 GOS scintillator with 1:1 fiber optics plate
Microfocus X-ray tube
KEVEX PXS10
45-130 kV
0.5 mA
53° beam angle
7-100 µm focal spot
Micro-CT system

## Slide 27
Trabecular microstructure of a child bone from the Anthropology Museum of UNIBO (voxel size: 10 mm).
Analysis of human skeletal remains

## Slide 28
X-ray CT images of a curved pendant:
a) 3D rendering;
b) internal section;
c) coronal slice, showing details of granulation and filigree decorations.
X-ray CT images of a circular pendant: a) coronal plane sectioning the 3D rendering;
b) crescent moon decoration;
c) star decoration.
PUNIC NECROPOLIS OF THARROS – CAPO SAN MARCO (SARDINIA, ITALY)
Micro-CT analysis of silver jewelry (7th-6th century BCE)

## Slide 29: Examples of case-studies
Analysis of medium-size artefacts

## Slide 30
CT system for medium sized-object

## Slide 31
Vertical axis
Flat panel
Vertical axis
Physik Instrumente (PI)
Model: M413.3PD
Range: 30 cm
Step: 1/10 micron
Physik Instrumente (PI)
Model: M413.3PD
Varian
Model: PS2520D
Pixel: 127 micron
Area: 25 cm x 20 cm
CT system for medium sized-object

## Slide 32
CT analysis of 4 animal mummies from the Archaeological Museum of Bologna.
CT analysis of Egyptian animal mummies

## Slide 33
Mummy of a cat
cm. 28
Unknown provenance
Ptolemaic - Roman period
Palagi Collection, EG 2039
Cat mummies represented a very common votive offering to Bastet, a goddess with a feline head.
CT analysis of Egyptian animal mummies

## Slide 34
Cat mummy (EG 2039)
CT analysis of Egyptian animal mummies

## Slide 35
Hawk mummy wrapped in linen bandages
cm. 28 x 6,5
Unknown provenance
Late Period-Ptolemaic Period
Palagi Collection, EG 2050
The falcon-like god Horus, closely related to the concept of royalty, is one of the most important deities for the ancient Egyptians.
This hawk mummy, covered only by a few layers of bandages that leave the head uncovered, appears intact.
CT analysis of animal mummies

## Slide 36
CT analysis of Egyptian animal mummies

## Slide 37
CT analysis of Egyptian animal mummies

## Slide 38
37 x 10 x 19.5 cm
Cat-shaped wooden coffin (Egyptian Collection of the Archaeological Museum of Bologna).
CT analysis of Egyptian animal mummies

## Slide 39
The Lilibeo Project
PARTNERS:
Centro Fermi
Bologna University & INFN
Tor Vergata University
Scuola Normale Superiore
University of Geneve
Trapani and Marsala Regional Pole for Cultural Sites
Regional Archaeological Museum «Lilibeo» (Marsala)
AIM OF THE PROJECT:
To study, through non-invasive methodologies, the characteristics of some finds preserved at the Lilybaeum Museum.

## Slide 40
The Lilibeo Project
Punic Ship
Roman Ship
Urban and Funerary wing

## Slide 41
CT analysis on-site
BABY-BOTTLES AND RATTLES
PLASTIC VASES
3th century B.C.

## Slide 42
CT analysis on-site
Black-glass aryballos (30×23×41 mm), late 4th – 3rd century B.C.
Polychrome glass alabastron (23×24×87 mm), late 4th – 3rd century B.C.
Blown glass balsamarium (height: 90mm), 1st century A.D.

## Slide 43
CT analysis on-site

## Slide 44
CT analysis on-site
Axial slices

## Slide 45
CT analysis on-site

## Slide 46
CT analysis on-site
Polychrome glass alabastron

## Slide 47: Examples of case-studies
CT analysis of large artefacts

## Slide 48
Vincenzo Coronelli
(1650-1718 )
Pair of terrestrial and celestial globes by Coronelli
Marciana National Library (Venice)
The Coronelli’s celestial globe at Marciana Library

## Slide 49
Transfer of the CT system on site
Marciana National Library in Venice

## Slide 50
C10900D – Hamamatsu –
Solid State Detector + CsI:TI scintillator
12 x 12 cm2
100 µm pixel
SMART EVO 200 D – Yxlon –
50-200 kV
0.5 – 6 mA
1 mm focal spot
Energy
150 keV
Current
2 mA
Resolution
200 μm
Fast Acquisition 3min x CT
Flat Panel Detector
X-Ray Tube
≈ 3.2 m
On-site experimental set-up

## Slide 51
Tile scanning
CT analysis of the globe
≈ 200 detector positions
3 minutes for each one
10 hours
180000 partial radiographs

## Slide 52
Poles
North Pole
South Pole
- wooden polar axis
- 7 internal circles
7 groups of 4 perpendicular wooden boards
- 2 polar pivots
- Metal nails
Results of the CT analysis

## Slide 53
Elements of the inner structure
Structural elements of the globe
Wooden elements on the surface

## Slide 54
The African wooden statue at Pigorini Museum
African wooden statue kept at the Luigi Pigorini Museum of Prehistory and Ethnography in Rome.
It represents an anthropomorphic idol believed to have magical power.
It is carved from a single piece of wood and has a lot of metal nails in the torso for a votive function.
Height: 120 cm
Second half of the 19th century

## Slide 55
In 2014 the Metropolitan Museum of New York asked the Pigorini Museum for the loan of this statue for an exhibition on African Art.
Conservators at the Pigorini Museum were concerned about some parts of the statue they considered fragile and critical, thus potentially subject to fracture and detachment especially during trasport from Rome to New York.
The African wooden statue at Pigorini Museum

## Slide 56
Details of the beard and of the so-called power-pocket in the abdomen of the statue: it consists of a bolus supporting a large shell and hiding an inner cavity with magical objects (herbs, stones, shells, etc.).
They have been shaped with a moldable material consisting of an oleo-resin mixed with kaolin, quartz and vegetable matter.

## Slide 57
A double line of metal pins deeply embedded into the wood offers firm support for the beard.

## Slide 58
Axial section of the abdomen showing the inner cavity behind the bolus.

## Slide 59
Four metal pins enclose the bolus of the so-called «power pocket».

## Slide 60
A polygon mesh of the surface obtained from the 3D volume allowed the scientists at the Metropolitan Museum of Art to design and build a custom-made crate with a molded interior for the safe transportation of the statue.

## Slide 61
X-ray Computed Tomography of the ancient globe by Egnazio Danti at Palazzo Vecchio – Florence (2004)
The Municipality of Florence decided to set up an important diagnostic campaign for this masterpiece. Besides the cleaning of the surface, which had become brown, the project also involved an exploration of the nature and condition of its inner structure. It was therefore decided to perform a CT scan.
The terrestrial globe by Egnazio Danti

## Slide 62
The Map room (“Sala delle Carte geografiche”) within Palazzo Vecchio, with the ancient large globe created by Egnazio Danti around 1567, on assignment of Cosimo I de’ Medici, duke of Florence.
The terrestrial globe by Egnazio Danti

## Slide 63
On the left: the X-ray tube;
in the middle: the globe on the turntable;
on the right: the detector and the translation axes (31000 radiographs).
The experimental set-up

## Slide 64
Picture of the experimental set-up: the detector on the moving axes on the left, the globe on the rotating platform in the middle, and the tube on the vertical moving axis on the right.
The terrestrial globe by Egnazio Danti

## Slide 65
Rendering of the 3D volume obtained by the CT reconstruction. It is clearly possible to see the entire inner structure, consisting of a central axis, 8 equatorial bars, 8 bars as 2 tetrahedrons and 30 meridians.
The terrestrial globe by Egnazio Danti

## Slide 67
The globe is no more a perfect sphere; it collapsed about 10 cm
30 meridians,
each 12° far
Calculated weight of iron:
TOTAL: ~608 Kg
INTERNAL: ~350 Kg
The globe is made mainly by iron
The terrestrial globe by Egnazio Danti

## Slide 68
Conclusions
CT is a versatile technique that can be applied to a variety of objects of different size and made of different materials.
The availability of mobile CT systems expands the number of case studies in which tomography can be applied.
Moreover, it gives us the possibility to work in close contact with restorers and conservators in the place where archaeological findings and works of art are located.

## Slide 69
Thank you for your attention!
Maria Pia Morigi
Department of Physics and Astronomy «Augusto Righi»
University of Bologna & INFN CHNet
Viale Berti Pichat, 6/2
40127 – Bologna
Tel.: +39 051 2095085
mariapia.morigi@unibo.it